Internal Memo no. 912/161– construction Date: 19-10-2023

Subject: Guidelines for ordering Adhesive for Tiles/Granite fixing works.

Keywords: Adhesive for Tiles, Granite fixing, Flooring & wall cladding

1. Adhesive for fixing of tiles and granite for vertical surfaces and below lentils has been standardized.
2. Sites to use:

|  |  |  |  |  |
| --- | --- | --- | --- | --- |
| Sl. No.  | Description of item | Details of use | SKU no.  | Appx. Cost |
| 1 | MYK Laticrete 335 Superflex multipurpose floor and wall adhesive - Available in 20 kg & 50 kg bags. | For Wall cladding - both internal & external. | CHEM5982-Chemical-MYK Laticrete-335 Super Flex Adhesive-Misc-Nos | Rs. 956/- per 20 kg bag.Rs. 2,006/- per 50 kg bag. |
| 2 | Ultratech tilefixo NT - Available in 25 kg bag. | – Do - | CHEM3732-Chemical-UltraTech Tilefixo NT-Misc-Nos | Rs. 620/- per 25 kg bag. |
| 3 | Adhesive for flooring - MYK Laticrete 305 Grey - Available in 20 kg bag. | For Tile & Granite flooring purpose only. | CHEM6602-Chemical-Tile Adhesive-20kgs-Nos | Rs. 266/- per 20 kg bag. |
| 4 | Square Notch Trowel | For maintaining thickness of adhesive | TOOL9464-Tools-Notched Trowel-Nos | Rs. 300/- each. |

Notes:

1. The specified thickness of these adhesives is 6mm (with a tolerance of +/- 2mm) and the coverage area is 35-40 sft per 25kgs bag.
2. Square notch trowel must be used.
3. In case the **plastered surface is uneven** plastering to be corrected before use of adhesive.
4. Plastering to be roughened to receive granite/tile.
5. Purchase to maintain adequate stock.
6. Use of araldite to be eliminated (or minimised). Do not use araldite for making rough surface behind the tile or granite.

Soham Modi